TUNNEL SUSPENSION SYSTEM

LH + HPS  |  Threaded eye • Grade 8.8 rod • Drop-in anchor

Complete suspension component packages in M8 and M16, with a galvanized DIN 582 eye, galvanized DIN 976 threaded rod and a choice of drop-in anchor. Intended application: overhead suspension in tunnel environments, subject to project-specific anchor design and verification.

Package overview

| Package | Size | NFG article | Rod length | Anchor options |
| --- | --- | --- | --- | --- |
| LH + HPS 1 | M8 | 990012858 | 150 mm | HE-A4 / HE-NS |
| LH + HPS 2 | M16 | 990012859 | 150 mm | HE-A4 / HE-NS |

Illustration is schematic; installation and load capacity must be assessed for the actual rock substrate. The supplied reference document includes concrete-anchor dimensional diagrams.

Components & materials

| Component | M8 article | M16 article | Specification / finish |
| --- | --- | --- | --- |
| LH eye | 14480800000205 | 14481600000205 | DIN 582 • C15 • HDG, EN 10684 |
| HPS threaded rod | 13370801500205 | 13371601500205 | DIN 976 • Class 8.8 • HDG, EN 10684 |
| HE-A4 drop-in anchor | HEA4M08 | HEA4M16 | Stainless steel A4 |
| HE-NS drop-in anchor | HENSM08 | HENSM16 | Steel • Atlantis coating (described as similar to HDG) |

LH eye — dimensions and stated maximum loads

| Parameter | M8 | M16 |
| --- | --- | --- |
| h | 36 mm | 62 mm |
| b | 13 mm | 27 mm |
| d2 | 36 mm | 63 mm |
| d3 | 20 mm | 35 mm |
| d4 | 20 mm | 35 mm |
| k | 8 mm | 14 mm |
| Max load at 0° | 0.14 tonnes | 0.70 tonnes |
| Max load at 45° | 0.10 tonnes | 0.50 tonnes |

HPS threaded rod

| Parameter | M8 | M16 |
| --- | --- | --- |
| Thread | M8 | M16 |
| Length | 150 mm | 150 mm |
| Minimum breaking load | 29.2 kN | 125 kN |

Drop-in anchor — source dimensions

| Parameter | M8 × 30 HE-A4/HE-NS | M16 × 65 HE-A4/HE-NS |
| --- | --- | --- |
| df | 9 mm | 18 mm |
| hef | 30 mm | 65 mm |
| h1 | 33 mm | 70 mm |
| hmin | 80 / 100 mm | 130 mm |
| hnom | 30 mm | 65 mm |
| d0 | 10 mm | 20 mm |
| L | 30 mm | 65 mm |

Reference standards and documentation

DIN 582 — lifting eye nuts / eyes • DIN 976 — threaded rods • EN ISO 10684 — hot-dip galvanized fasteners. 
• ISO 898-1 — Mechanical properties of fasteners made of carbon steel and alloy steel
For the drop-in anchors, the source refers to Declarations of Performance (DoP) and separate technical documentation, without attaching them.

Design and installation considerations

Select the drop-in anchor and embedment based on verified rock conditions, borehole geometry and the anchor manufacturer’s instructions.

Confirm the permissible assembly load, including the eye, threaded rod, anchor, load direction and safety factors; component load figures are not a verified system capacity.

Verify thread engagement, corrosion exposure, compatibility of materials and any project-specific tunnel requirements before installation.

Product components shown for illustration. NFG LH marking and final packaging specifications to be confirmed.